## Slide 1: An Investigation of Thermal-Structural Coupling Problem of Dry Friction Clutches and Environmental Impact
By
Nasr Abulameer Jabbar
Supervised By
Prof. Dr. Ihsan Y. Hussain
Prof. Dr. Oday I. Abdullah

## Slide 2: Objectives of The Research
Develop a new numerical solution of the thermal-structural coupling problem of friction clutch systems using FEM for different configurations.
Study experimentally the negative effect of emissions of friction clutches during its work on the surrounding environment.
Develop the existing test rig of dry friction clutches to study experimentally the thermal performance under different working conditions.
Enhance the analytical solution to calculate the temperature during the sliding period.

## Slide 3: The Scientific Originality
The Numerical model and numerical simulation of the coupling problem.
The verified experimental work for different configurations of clutches.
Find the magnitude of emissions of friction clutches on the environment.
The proposed analytical solution.

## Slide 4: The work principle of dry friction clutch :

## Slide 5: The Thermal Effect During the Working Stages of the Clutch

## Slide 6: Literature Review
Thermal and thermoelastic problems in dry friction clutch:
A comprehensive review, Heat Transfer, Wiley Periodicals LLC.
Writing the CH.2 in a different style.

## Slide 7
Plan of research
Two-dimension
models
Numerical solutions
Three-dimension
model
Analytical solution
Experiment solutions
Thermal tests by clutch rig
Environmental Impact

## Slide 8: Functionally graded material

## Slide 9: Numerical Solution: Frist model (2-D model)
Figure (1): The model with FGM layers and boundary conditions for clutch system (a). the model. (b) the variation of layers in friction lining. (c) the dimensions of layers.

## Slide 10
The Material | sic | Al
Friction Coefficient | 0.6 | 0.47
Modulus of Elasticity Pa | 4 e+11 | 6.96 e+10
Specific Heat J/kg.K | 750 | 923.5
Thermal Conductivity W/m.K | 120 | 160
Density kg/m3 | 3100 | 2770
Type of layer | No. of layer | Volume proportion of AL |  | 
 |  | K=0.5 | K=1 | K=5
3 Layer | Layer 1 Layer 2 Layer 3 | 57.73% 81.65% 100% | 33.333% 66.67% 100% | 0.4115% 13.1687% 100%
4 Layer | Layer 1 Layer 2 Layer 3 Layer 4 | 50% 70.7% 86.6% 100% | 25% 50% 75% 100% | 0.0977% 3.125% 23.73% 100%
5 Layer | Layer 1 Layer 2 Layer 3 Layer 4 Layer 5 | 44.72% 63.245% 77.46% 89.44% 100% | 20% 40% 60% 80% 100% | 0.032% 1.024% 7.776% 32.766% 100%
Table (2): The control factors of FGM material.
Table (1): The material properties of Sic, and Al materials.

## Slide 11
Figure (2): The temperature distribution at mean radius
between all layers' group of friction lining
and axial cushion.
Figure (3): The temperature distribution with number
of layers at different values of power- law variation (K)
and inner radius, mean radius, and outer radius.

## Slide 12
Figure (4): The comparison between a. pure Sic, b. pure Al, and c. best result at (3 Layers, k=0.5).

## Slide 13: Numerical Solution: Second model (2-D model)
Numerical simulation of dry friction clutch thermal behavior with different friction materials, 8th Engineering and 2nd International Conference for College of Engineering.

## Slide 14
The Material | HCC | G95 | LUK | Tiger
Friction Coefficient | 0.45 | 0.55 | 0.3 | 0.3
Modulus of Elasticity GPa | 310 | 305 | 490 | 420
Specific Heat J/kg.K | 900 | 935 | 1010 | 1780
Thermal Conductivity W/m.K | 33 | 24 | 0.4378 | 0.726
Density kg/m3 | 1950 | 1870 | 1734 | 1570
Table (3): Friction Material Properties
Table (4): The Studied Parameters
Inner disc radius, ri = 0.0632 m.
Outer disc radius, ro = 0.0885m.
Friction material thickness, tc = 0.0032 m.
The thickness of the axial cushion, ta = 0.0016 m.
The number of engagements =1.
Torque Capacity = 111 N.m.
Friction surfaces number, np = 2.
Maximum angular slipping speed, ω = 293 rad/s.
Initial temperature, Ti =300 K.
The slip time ts= 0.4 s

## Slide 15
(c)
(a)
(b)
(d)
Figure (5): Friction clutch element temperature distribution at 0.2 s with (a) Luk lining, (b) Tiger lining, (c) G95 lining, and (d) HCC lining.

## Slide 16
(a) (b)
(c)
Figure (6): Different radii of friction clutch elements and their corresponding temperature distribution in the cross section are labeled (a) ri, (b) rm, and (c) ro.

## Slide 17: Numerical Solution: 3-D model
Figure (7): Schematic Diagram of the Stages of Thermo-Elastic Formation
Figure (8): 3D FE model of clutch system.

## Slide 18: Analytical solution
Figure(9): Diagrammatic sketch demonstrating the heat created at a single-plate friction clutch rubbing surfaces and its flow.

## Slide 19
The governing equation
……………..1
Equivalent principle of FGM properties
……………………………..2
………………3
…………………………..………..4

## Slide 20
a. FGM _equivalent properties b. FGM_3 Layers
Figure (10): The numerical examination of equivalent properties approach.
Dimensionless forms

## Slide 21
Figure (12): Temperature distribution at the dry clutch's
component interface for various speeds,
torque of 126 N.m., and slip time of 0.4 sec.
Figure (11): Temperature distribution at the dry clutch's component interface for various loads at 5300 rpm and 0.4 sec of slip

## Slide 22
Figure (13): temperature distribution at the dry clutch's component interface for various slip periods, with a velocity of 5300 rpm and a constant torque of 126 Nm.
Figure (14): Temperature distribution at the dry clutch's
component interfaces for various materials when
the torque is 126 Nm and the speed is 5300 rpm

## Slide 23
Experimental work: Part 1
In experimental part 1 will study the effect of these kinds of friction materials on the behavior of the sliding system
Figure (15): clutch test rig.

## Slide 24: Experimental work: Part 2
Figure (16): The test rig of environmental impact

## Slide 25
Thank you
for your listening